## Slide 1: RISERS

## Slide 2: Mainly used for
Reducing the shrinkage problem in the casting.
Promotes direction solidification

## Slide 3: Comparison b/w open & blind riser
Open Riser
Having open top
Feeding force is gravity force and atm. Pressure
Connected at the top/on the side at the parting line
Cylindrical in shape
Comparatively larger
Blind Riser
Closed at the top
Only gravity force responsible for feeding
Can be placed at any position in the mold
A rounded cavity
Smaller in size

## Slide 4: Continue…..
Due to rapid cooling rate insulating & exothermic compounds is recommended
Height depends on height of molding box
Easy to mold
Slow cooling rate due to surrounding molding sand
Height depend on feeding requirement
Difficult to mold

## Slide 5: Casting Defects
Deviation of casting from its requirements
Flaws- due to improper appearance

## Slide 6: Classification of Defects
Visually expectable
Exists under surface
Discovered by testing

## Slide 7: DEFECTS CAUSED BY PATTERN & MOLDING BOX
MISMATCH/MOLD SHIFT
Mismatch of top & bottom part of the casting

## Slide 8
2) Variation in wall thickness of casting-
due to oversize dimensions
3) Fins, Fash and strain-
occurs at parting line.
mold movement makes casting thicker
4)crush-
displacement of sand during mold closing

## Slide 9: 2. DUE TO IMPROPER SAND CASTING
BLOWHOLES-
smooth round holes
visible at surface – open holes
May occur in cluster /one large smooth depression

## Slide 10: Causes of blow holes
Excess moisture in sand
Improper baked and inadequately vented core.
Presence of gas producing ingredients
Extra hard ramming of sand

## Slide 11
2) DROP
mixing of sand into the molten metal
Causes-
Low green strength
Low mold hardness
Insufficient reinforcement

## Slide 12
3) SCAB-
penetration of molten metal in sand
Causes-
Too fine sand
High moisture content sand
Local heating
Uneven ramming

## Slide 13
4) PIN HOLES/POROSITY-
No of small holes present on casting surface
Causes-
High moisture in sand
Metal-mold reaction

## Slide 14
5) HOT TEARS-
internal/ external cracks with ragged edges

## Slide 15
Causes-
High sulphur content
Low pouring temperature
very hard ramming
high dry & hot strength
Too much shrinkage

## Slide 16
6) MISRUN-
Incomplete filling of casting before solidification
Causes-
Too cold metal
Too thin casting
Too small gates

## Slide 17
7) COLD SHUTS-
Inability of fusing metal coming from 2 gates

## Slide 18
8) SLAG HOLES
9) SHRINKAGE DEFECTS

## Slide 19: DEFECTS DUE TO MOLTEN METAL
SAND CUTS & WASHES-
Flow of molten metal over mold /core
Causes-
Soft ramming
Insufficient draft
Improper gating system

## Slide 20
WARPAGE
HARD SPOTS
SWELLS
INCLUSIONS
FUSION

## Slide 23: MELTING FURNACES
used to melt the metal
Remelting created by combustion of fuel, electric arc, electric resistance
Blast furnace for melting
Electric arc furnace for remelting

## Slide 24: SELECTION CRITERION
cost
Type of metal to be melted
Quality required
Flexibility
Melting efficiency
Degree of control

## Slide 25: Furnace for melting
Grey cast iron
  Cupola
  Air (reveberatory)
  Rotary
  Electric arc
  Steel
  Open hearth
  Electric
  converter

## Slide 26
Non-ferrous metals
  Crucible
  Pot
  Air
  Rotary
  Induction
  Electric arc

## Slide 27: CUPOLA FURNACE
Melt scrap metal
Economical for gray, nodular, malleable cast Fe
Fuel used
  high grade low sulphur coke
  Anthracite coal
  Or C- briquettes

## Slide 28: CONSTRUCTION
Cylindrical shell of 6-10 mm thick plate
Tuyeres dimensions- 50mm* 150mm
Upto 75cm dia cupola 3-4 tuyeres used

## Slide 29: CONSTRUCTION
Normal air pressure
  12”-16” water gauge for small cupola
  16”-35” for large
Capacity- 1-15 tons/heat
Height – 2.5 m - 4 m & 6 m
Inside dia- 75 cm – 2.5m

## Slide 32: CUPOLA OPERATION
PREPARATION OF CUPOLA
  Cleaning repairing operation
  Patching-(2 parts ganister/silica & 1 part fireclay)
  Cupola block-
    Si - 52% -62%
    Al- 31%-43%
    Titania- 1.5%-2.5%
    Fluxing oxides- 3%- 6%

## Slide 33
LIGHTNING THE FIRE
  Started 3 hrs before working
  Can be lighten by-
    Electric spark ignitor
    Gas torch

## Slide 34
CHARGING OF CUPOLA-
Adding layers of flux ,iron & coke
Commonly used flux-
  CaCO3
  Na2CO3
  CaF2
  CaC2
  Avoid large amount of flux
  Amount – 2% - 4% by weight of metal
  Fuel used
    Low S coke, anthracite coal & carbon briquettes

## Slide 35
Metal fuel ratio- 4:1-12:1
Metal charge consists
  Pig Fe -30%
  Scrap iron -30%
  Returns -40%

## Slide 36
MELTING
soaking period- 30 min
SLAGGING AND METAL TAPPING
collect slag
Collect metal into the ladle
DROPPING DOWN THE BOTTOM
Shut down the cupola

## Slide 37: ZONES OF CUPOLA

## Slide 39
WELL
Collect molten metal
SUPERHEATING COMBUSTION/ OXIDIZING ZONE
15-30cm above tuyere level
C, Mn, Si react with O2
Amount of heat generated- 14452 BTU/ pound
Temperature 1550 -1850 degree C

## Slide 40
REDUCING ZONE/ PROTECTIVE ZONE
Temperature- 1200 degree C
C + CO2  2CO - heat(2910BTU)
MELTING ZONE
90cm above coke bed
Temperature- 1600 degree C
3Fe +2CO  Fe3C + CO2

## Slide 41
PREHEATING ZONE
Melting zone – bottom of charging door
Temperature about 1100 degree C
STACK ZONE
Exhaust
Stack gases contains
Nitrogen-76%, 12% CO2, CO